###### Case History

………………………………………………………………………………………………

Project				CF 208, Salt Lake City Building

Industry			           Building Residential

Location			           Kolkata

Year of Completion		 2006

Consultant	Mr. Sanjiv J. Parekh,

##### M/S S.P.A. Consultants

53,Justic Chandra Madhab Road

Kolkata-20

Product	Nitowrap EP (CF), Conbextra EP10, Lokfix S, Nitowrap 410, Nitoprime 30,Rendroc FC

# Applicator  	Mr. P.V. Raman

# M/S NuTech Engineering

# 197, Park Street, Kolkata-17

………………………………………………………………………………………………

Surface preparation & cleansing

### Mixing

### Surface Preparation

## Application Of Nitoprime 30

## Application Of Nitowrap 410 and Nitowrap CF

### Rolling

## Spraying Sand

### Customer Requirement:-

- The cured concrete samples filed when tested during the construction of a residential building at Salt Lake City, A G+4 structure.

- Mr. Sanjiv J. Parekh, of M/s S.P.A Consultants, Kolkata was consulted for the suggesting a remedial measure

- It was recommended by the consultant to go for necessary NDT tests.

- Inference was made that 17 numbers of columns were having the compressive strength below M10 as per the report submitted by the testing agency, These results were found to be below acceptable engineering parameters and the quality of the cement used was found to be inferior.

- The client requirement was to counter this problem and offer him the suitable technology/solution.

- The owner was not interested for time consuming conventional techniques.

- Fosroc Chemicals (India) Pvt. Ltd., was then assigned to some suitable measure to counter the same.

- After discussions with the consultant it was finally decided that Nitowrap EP (CF) carbon fiber wrapping system need to be carried out for strengthening the 17 columns.

#### Proposed Solution:-

- The 17 columns were marked and thoroughly examined for undulations and soundness.

- The nozzles were fixed thought the column and were grouted after proper mixing with mechanical mixer using Conbextra EP10 to make the column strong and void free.

- Columns were thoroughly cleaned by air blowers and undulations were properly taken care of by mechanical chipping machines to make the surface smooth and even by the use of Lokfix S to fill various gaps.

- A layer of Rendroc FC was applied to make the surface smoother, so that the fiber will be thoroughly adhered to the column surface.

- A layer of Nitoprime 30 was then applied and subsequently allowed to dry for 12 hours.

- Nitowrap EP (CF) carbon fiber wrapping system was then applied to columns with prior application of Nitoprime 410 ensuring proper over lapping as per the technical datasheet and layer of saturant Nitoprime 410 is applied.

- Before the saturant is completely dried a layer of sand is to be sprayed/sprinkled to provide a mechanical key that will help for future plastering.